## Slide 1: Water model experiments on the influence of the phase distribution in the SEN considering varying operating conditions
Maria Thumfart, Gernot Hackl, Wolfgang Fellner
05.10.2021

## Slide 2: Contents
Motivation
Experimental setup
Scaling of the volume flow rates
Measurement parameters and material properties
Experimental results
Conclusion

## Slide 3: Motivation
argon injection common practice
resulting phase distribution subject of investigation
phase distribution in the SEN strongly influenced by conditions at stopper tip
measurements of the phase distribution near the stopper tip in a continuous caster challenging
accessible parameters at the steel plant
  stopper lift
  stopper feeding pressure
 influence of the phase distribution in the SEN on stopper lift and stopper pressure evaluated in a 1:3 watermodel

## Slide 4: Experimental setup: 1:3 water model

## Slide 5: Scaling of the flow rates
Froude number
Volume flow rates according to Froude similarity
Ideal gas law
Resulting air flow rate
Rough estimate: ferrostatic pressure stopper tip
Air flow rate assuming m

## Slide 6: Experimental parameters
Goal: achieve different phase distributions at the same water and air flow rate
Parameters influencing phase distribution in the SEN:
  water flow rate
  air flow rate
  time derivative of the air flow rate (increasing and decreasing)
  wetting behaviour wall material stopper tip and SEN top
Material | water flow rate | air flow rate ramps | 
 | l/min | l/min | l/min
acrylic glass | 1.92 | 0.5 – 5.8 | 5.8 – 0.5
 | 1.66 | 0.5 – 5.8 | 5.8 – 0.5
petrol jelly | 1.66 | 0.5 – 5.8 | 5.8 – 0.5
paraffin | 1.66 | 0.5 – 5.8 | 5.8 – 0.5
Material | contact angle
 | °
acrylic glass dry | 90
acrylic glass prev. wet | 78
petrol jelly | 93
paraffin | 101

## Slide 7: Example measurement: acrylic glass; water flow rate 1.92 l/min
Symbols
   stopper feeding pressure in Pa
   stopper position in mm
   air flow rate in l/min
Frame rate: 1 fps
Videos used to detect changes in the phase distribution
Example contains all four detected phase distributions

## Slide 8: Example: Snapshots
Bubble threads
Foam
intermediate level, air near wall
intermediate level, air centered

## Slide 9: Example measurement: acrylic glass; water flow rate 1.92 l/min
Symbols
   stopper feeding pressure in Pa
   stopper position in mm
   air flow rate in l/min
Frame rate: 1 fps
Videos used to detect changes in the phase distribution
Example contains all four detected phase distributions

## Slide 10: Example: raw data acrylic glass; water flow rate 1.92 l/min
(a)
(b)
(c+d)
(c+d)
(b)
(a)
(b)
(b)
(c+d)
(c+d)
calculated from feeding pressure and air flow rate
smoothing length 5s
average of three sensor signals in each measurement plane
no Argon: measured averaged pressure single phase flow

## Slide 11: Comparison stopper tip pressure
stopper tip pressure strongly influenced by phase distribution
influence of water flow rate on stopper tip pressure only minor
petrol jelly
paraffin
acrylic glass
acrylic glass

## Slide 12: comparison stopper position
smoothing length 5sec
changes of phase distributions visible in stopper lift
acrylic glass
acrylic glass
petrol jelly
paraffin

## Slide 13: Conclusion
four different phase distributions detected
hysteresis effect of the phase distributions was shown
each phase distribution change affects
  stopper lift
  pressure at the stopper tip
  pressure in the SEN top
wetting conditions at the stopper tip and SEN top show influence on phase distributions
Notes: (mean and fluctuation magnitude)

## Slide 14: References
B.G. Thomas, steel research int., Vol. 89, 2018, 1700312
H. Yang et al., Metals, Vol. 11, Iss. 1, 2021, https://doi.org/10.3390/met11010116
T. Hbiki et al., International Journal of Heat and Mass Transfer, Vol. 47, 2004, p. 1847-1862
M. Ishii et al., International Journal of Multiphase Flow, Vol. 30, 2004, p. 779-801
O.N. Kashinsky et al., International Journal of heat and Mass Transfer, Vol 49, 2006, p. 3717-3727
D.N. Mena, Inlet-induced effects on vertical co-current downward air-water two-phase flow, Master-Thesis, The Pennsylvania State University, 2016
M. Milan et al., International Journal of Multiphase Flow, Vol. 56, 2013, p. 126-137
S. Qiao et al., Nuclear Engineering and Design, Vol. 312, 2017, p. 375-388
M. Saeedipour and S. Pirker, Proc. 9th Int. Con. on Modelling and Simulation of Metal. Proc. Steelmaking, STEELSIM 2021, Vienna, Austria, 2021
S. R. Higson et al., Improvement in cast product quality by the visualization and control of the steel flow pattern in the tundish pouring nozzle (SEN/SES), EUR 21247 EN
N. Terzija et al., Flow Measurements and Instumentation, Vol. 22, 2011, p. 10-16
H. Bai, B. G. Thomas, Metallurgical and Materials Transactions B, Vol. 32, 2001, p. 269-284
S.R. Higson et al., Improvement in cast product auality by th evisualisation and control of the steel flow pattern in the tundish pouring nozzle (SEN/SES), EUR 21247 EN, 2005
K. Thimmel et al., 2018 IOP Conf. Series: Materials Science and Engineering, Vol. 424, 012032, doi:10.1088/1757-899X/424/1/012032
K. Timmel et al., Metallurgical and Materials Transactions B, Vol. 46B, 2015, p. 700-710
M. Ratajczak et al., 2017 IOP Conf. Series: Materials Science and Engineering, Vol. 228, 2017, 012023, doi:10.1088/1757-899X/228/1/012023
J. Eck, Development of systematic measurement on liquid metal, Master-Thesis, Lulea University of Technology, 2019
S. Hänsch et al., Chemical Engineering Science, Vol. 244, 2021, ISSN 0009-2509
G. Tryggvason et al., Physics of Fluids, Vol 25, 2013, https://doi.org/10.1063/1.4793543
ANSYS Fluent User’s Guide, 2021 R1, p. 2511-2792
M. Thumfart, Modellierung des Wasserbadmodells der Stranggussanlage, Diploma-Thesis, JKU Linz, 2008, p. 153

## Slide 15: Thank you!