## Slide 1: „Development of galvanized and galvannealed 3rd Gen. AHSS“ Effect of Si and Al on retained austenite stabilization during Q&P and galvannealing process
Matthias Wallnera,c, K. Steinederb, R. Schneidera, C. Sommitschc
aDepartment for Materials Technology, University of Applied Sciences Upper Austria, Wels, Austria;
bResearch & Development and Innovation, voestalpine Steel GmbH, Linz, Austria;
cInstitute of Material Science, Joining and Forming, Graz University of Technology, Graz, Austria

## Slide 2: Introduction
TE [%]
0
10
20
30
40
50
60
0
400
600
1000
200
800
1200
TS [MPa]
HSS
(HSIF, Isotrop,
BH, HSLA, CMn)
mild steel
(IF, LC)
1st Gen. AHSS
(TRIP, DP, CP)
1400
2nd Gen. AHSS (TWIP)
3rd Gen. AHSS
(Medium-Mn, TBF, Q&P)
martensitic steel

## Slide 3: Introduction
TE [%]
0
10
20
30
40
50
60
0
400
600
1000
200
800
1200
TS [MPa]
HSS
(HSIF, Isotrop,
BH, HSLA, CMn)
mild steel
(IF, LC)
1st Gen. AHSS
(TRIP, DP, CP)
1400
2nd Gen. AHSS (TWIP)
3rd Gen. AHSS
(Medium-Mn, TBF, Q&P)
martensitic steel
+ high product of TS×TE
(crash safety)
+ balance global to local ductility
(deep drawing to bending)
- galvanizeability (selective surface oxides)
- slow galvannealing (Fe-Zn) reactions
- poor weldability due to LME
Due to Si↑

## Slide 4: Experimental procedure
C
γ
α‘1(Tq)
CR
α‘1
αB
α‘2
RA
RA…retained austenite ; α‘1…tempered martensite
αB…bainitic ferrite; α‘2…fresh martensite
GA
T[°C]
t[s]
Ac3
MS
Ac1
Tq
Small scaled steels | C [%] | Mn [%] | Si [%] | Al [%] | Ac1 [°C] | Ac3 [°C] | MS [°C]
0.2C-4Mn-1.5Si | 0.2 | 4 | 1.5 | 0 | 722 | 820 | 314
0.2C-4Mn-1.5Al | 0.2 | 4 | 0 | 1.5 | 738 | 885 | 334
-50K/s
400°C – 40s
480-560°C
(20s)
Aim:
Influence of a fully substitiution of Si by Al on
Carbide precipitation in α‘1
RA stabilisation to room temperature
RA stabilisation during GA
during Q&P with subsequent GAlvannealing
Methods:
- Microstructure – SEM/EBSD
- Tempering behavior of martensite – derivation of rel. length change (dilatometer) & heat flow (DSC)
C
t[s]
Xphase
[vol.%]
Q1 vs. Q2
Zn
Inductor
T↑

## Slide 5: RA-Austenite stabilization during Q&P
T[°C]
t[s]
Ac3
MS
Tq
 | α‘1 [%] | αB [%] | α‘2 [%] | RA [%] | CRA[1] [wt.%] | PAGS [µm]
0.2C-4Mn-1.5Si | 60 | 9 | 10 | 21 | 0.79 | 5.5
0.2C-4Mn-1.5Al | 63 | 14 | 6 | 17 | 0.88 | 12.3
(RA; α‘1; α‘2)
230°C
270°C
(LeverRule)
400°C
40s
~60% α‘1
~60% α‘1
size
lath-like shape
X
y
→ Carbide precipitation during α‘1-tempering reduces C-partitioning → RA ↓
→ Influence of Si & Al on tempering behavior of α‘1?
1µm
1.5Si
1µm
1.5Al
[1] N.H. van Dijk; Acta Mater. 53 (2005) 5439–5447
M. Wallner, et. al., Mater. Sci. Tech. 37 (2021) 182-189

## Slide 6: Influence of Si vs. Al on carbide precipitaton in α‘1
Start of carbide precipitation
RX
Fe3C
Fe3C
RAdec
C-seg/
clust.
RAdec
εprec
Tempering of fully martensitic microstructure 10K/min
- Dilatometer – dl/dT (H1-H2) – carbide prec. = contraction & RA-decomposition = expansion
- Differential Scanning Calorimetry – heat flow (H1-H2)
H1 - H2
DIL: dl1/dT - dl2/dT
DSC: heat flow1 - heat flow2
T[°C]
t[s]
Ac3
MS
10K/min
10K/min
α‘ ~98%
600°C
600°C

## Slide 7: Influence of Si vs. Al on carbide precipitaton in α‘1
T[°C]
t[s]
Ac3
MS
Carbides spherolize, but most maintain needle shaped and coarse
Needle shaped carbides spherolize & accumulate at α‘1 lath & at PAG-boundarys
1.5Al Q&P+
GA560
θn
θsp
1µm
1µm
1.5Si Q&P
θn
1µm
1.5Si Q&P+
GA560
θacc
θsp
1µm
1.5Al Q&P
θn
εprec → Fe3C & coarsening
Start of carbide precipitation
RK
Fe3C
Fe3C
RAdec
C-seg/
clust.
RAdec
εprec
~ amount of carbides precipitate during partitiong??

## Slide 8: Influence of Si vs. Al on carbide precipitaton in α‘1
ART
A400
T[°C]
t[s]
Ac3
MS
10K/min
α‘ ~98%
~ amount of carbides precipitate during partitioning??
20K/s - 400°C – 40s
How much carbon precipitate already due to isothermal annealing at 400°C ?
400°C
Approximation of amount of C precipitation in α‘1
x%Al
x%Si

## Slide 9: Influence of Si vs. Al on RA during GA
T[°C]
t[s]
Ac3
MS
GA480
GA520
GA560
αB
αB + Fe3C
Fe3C (α‘1)
Pearlite
αB
αB + Fe3C
Fe3C (α‘1)
Pearlite
T↓ RA-decomposition effects
- Carbide precipitation Al > Si
- Bainite transformation Al > Si
T↑ RA-decomposition effects
- Perlite transformation Si > Al
T↓
T↑
→ Increasing the temperature stability of RA by Al due to retarding pearlite formation
P
α‘2
T[°C]
t[s]
Ac3
MS
Tq
10K/min
What happens with RA during tempering?
M. Wallner, et. al., Mater. Sci. Tech. 37 (2021) 182-189

## Slide 10: Influence of Si vs. Al on RA during GA
T[°C]
t[s]
Ac3
MS
GA480
GA520
GA560
αB
αB + Fe3C
Fe3C (α‘1)
Pearlite
αB
αB + Fe3C
Fe3C (α‘1)
Pearlite
T↓ RA-decomposition effects
- Carbide precipitation Al > Si
- Bainite transformation Al > Si
T↑ RA-decomposition effects
- Perlite transformation Si > Al
T↓
T↑
T[°C]
t[s]
Ac3
MS
Tq
10K/min
What happens with RA during tempering?
M. Wallner, et. al., Mater. Sci. Tech. 37 (2021) 182-189

## Slide 11: Conclusion
Q&P-process substitiution of Si by Al due to high carbide precipitation in α‘1 not sufficient
Only Si → high TS×TE after Q&P but increased decomposition of RA during GA
Only Al → low TS & work hardening, but increasing the thermal stability of RA during GA
→ For Q&P + GA process optimum Si:Al ratio required
T[°C]
t[s]
Ac3
MS
α‘-tempering
60%-α‘- + 40% austenite temp.
1.5Al
1.5Al αB↑
1µm

## Slide 12: Thank you for your attention!
Matthias Wallnera,c, K. Steinederb, R. Schneidera, C. Sommitschc;
aDepartment for Materials Technology, University of Applied Sciences Upper Austria, Wels, Austria;
bResearch & Development and Innovation, voestalpine Steel GmbH, Linz, Austria;
cInstitute of Material Science, Joining and Forming, Graz University of Technology, Graz, Austria
The authors sincerely acknowledge the support of the Austrian Research Promotion Agency (FFG) related to the frontrunner project No. 860188 “Upscaling of medium Mn-TRIP steels”.