## Slide 1: Structure-Property Relationship in Additively Manufactured High-Manganese Steels
High Manganese Steel Conference 2022
Dilay Kibaroglu, S. Amir H. Motaman, Christian Haase, Ulrich Krupp, Patrick Köhnen, Claudia Drebenstedt, Christian Hannemann, Thomas Hipke

## Slide 2: Content
Introduction
  Metal additive manufacturing
  Cellular materials
  Cellular and lattice structures
Alloy Design Approach
Modelling and Simulation of Mechanical Response
  Meso-structure modelling
  Crystal plasticity simulation
Lattice Structures
  Mechanical behaviour
  Optimization of cell design
Conclusion
Outlook

## Slide 3: Introduction
Metal additive manufacturing – Laser Powder Bed Fusion (LPBF)
Selective melting of thin layers of metal powder by means of a laser source
T. Özel, A. Altay, B. Kaftanoğlu, R. Leach, N. Senin, A. Donmez, Journal of Manufacturing Science and Engineering 142 (2020).
A.A. Antonysamy, J. Meyer, P.B. Prangnell, Materials Characterization 84 (2013) 153–168.
Notes: Additive manufacturing which is also known as 3D printing is a novel technique that enables layer by layer (additive) production of parts by utilising powder, wire or sheet as feedstock material.
Rapid alloy prototyping which is quite an advantage for alloy design purposes.
Epitaxial grain growth

## Slide 4: Introduction
Additive manufacturing of high-manganese steels (HMnS)
2nd generation AHSS  combination of strength and ductility
Activation of different deformation mechanisms by tailoring stacking fault energy (SFE) via alloy design approach
Promising alloy for additive manufacturing
Different properties than conventionally produced HMnS
  reduced elemental segregation and promotion of - and -martensite formation due to high cooling rates during AM process
  pronounced texture (along building direction)
  non-uniform grain morphology
LPBF
C. Haase, J. Bültmann, J. Hof, S. Ziegler, S. Bremen, C. Hinke, A. Schwedt et al., Materials (Basel, Switzerland) 10 (2017).
S.A.H. Motaman, C. Haase, International Journal of Plasticity 140 (2021) 102941.
microstructural heterogeneities
anisotropy in mechanical response
Notes: lead to anisotropy in mechanical response due to

## Slide 5: Introduction
Cellular materials
Porous microstructures which consist of solid and void networks - e.g. marine sponges, honeycombs, bones, metallic foams
Lattice structures
Differently from other cellular structures, topologically ordered 3D structures formed by repeating unit cells composed of network of struts which are connected at nodes
Sade Baron Inc, PW Sea Sponge. www.sadebaron.com/products/prime-wool-sea-sponge.
A.A. Saleh, C. Haase, E.V. Pereloma, D.A. Molodov, A.A. Gazder, Acta Materialia 70 (2014) 259–271.
Bones | Biology. www.ck12.org/c/biology/bones/lesson/Structure-of-Bones-BIO/.
C.T. Richard, T.-H. Kwok, Materials (Basel, Switzerland) 14 (2021).
T. Tancogne-Dejean, A.B. Spierings, D. Mohr, Acta Materialia 116 (2016) 14–28.
unit cell

## Slide 6: Introduction
Potential applications of lattice structures
mostly biomedical and aerospace
Examples: Energy absorbers, Vibration absorbers, Gas turbine engine fan blades, Wings, Heaters and heat exchangers, Biomedical implants
Advantages:
high energy absorption
programmable mechanical response through topology and cell design
T. Maconachie, M. Leary, B. Lozanovski, X. Zhang, M. Qian, O. Faruque, M. Brandt, Materials & Design 183 (2019) 108137.
C. Pan, Y. Han, J. Lu, Applied Sciences 10 (2020) 6374.
Biomedical
Aerospace
Metallic implants with a stiffness closer to that of bone and preventing stress shielding
Enabling the flow of body fluids by means of their porous structure
High strength-to-weight ratio
Thermal conduction / Heat dissipation

## Slide 7: Introduction
Additive manufacturing of lattice structures
Design freedom, geometries which are difficult to obtain by conventional manufacturing methods
Different cell shapes and sizes can be design by CAD software
B. Hanks, J. Berthel, M. Frecker, T.W. Simpson, Additive Manufacturing 35 (2020) 101301.
3.M.P. Magazine, A Solution for Laser-Beam Quality Analysis During Powder-Bed Fusion Production. www.3dmpmag.com/article/?/powder-bed-systems/laser/a-solution-for-laser-beam-quality-analysis-during-powder-bed-fusion-production.
High resolution (especially LPBF) enables the production of more complex designs with thin struts
  Laser spot size usually < 100 µm (Aconity Mini 82 µm)
Notes: Strut diameter which is twice the spot diameter was tried in a study - J.A. Harris, R.E. Winter, G.J. McShane, International Journal of Impact Engineering 104 (2017) 177–191.

## Slide 8: Alloy Design Approach
Controlling the dominant deformation mechanism and phase distribution through Al addition
P. Köhnen, S. Ewald, J.H. Schleifenbaum, A. Belyakov, C. Haase, Additive Manufacturing 35 (2020) 101389.
Changing deformation mechanism based on SFE (effect of different Al compositions)
as-deformed
HMnS - X30Mn22 + xAl (wt.%)
Power: 120 W
Scanning speed: 750 mm/s
LPBF
Notes: Al-0  TRIP accompanied by minor TWIP
Al-1  TWIP accompanied by minor TRIP
Al-5  In addition to dislocation glide, TWIP in the fcc phase

## Slide 9: Modelling and Simulation of Mechanical Response
Modelling of meso-structure (grain morphology and crystallographic texture) based on EBSD and XRD data  RVE generation by DREAM.3D
Physics-based constitutive crystal plasticity model based on continuum mechanics  DAMASK
Strain hardening curves
Flow curves
Representative Volume Element (RVE)
LPBF
Meso-structure Modelling
Crystal Plasticity Simulations
HMnS with 1 wt.% Al

## Slide 10: Modelling and Simulation of Mechanical Response
Meso-structure Modelling
Crystallographic orientation distribution
Grain shape-axis orientation distribution
EBSD IPF maps
S.A.H. Motaman, C. Haase, International Journal of Plasticity 140 (2021) 102941.

## Slide 11: Modelling and Simulation of Mechanical Response
Orthogonal to BD
Meso-structure Modelling
Parallel to BD
Mean grain size (area): 43.98 µm
Mean grain size (number): 15.12 µm
Effective grain size: 29.55 µm
Mean aspect ratio (area): 0.61
Mean aspect ratio (number): 0.57
Effective aspect ratio: 0.58
Mean grain size (area): 66.53 µm
Mean grain size (number): 17.04 µm
Effective grain size: 41.79 µm
Mean aspect ratio (area): 0.36
Mean aspect ratio (number): 0.42
Effective aspect ratio: 0.39

## Slide 12: Modelling and Simulation of Mechanical Response
Four principal modules for RVE generation by DREAM.3D
equivalent ellipsoidal grain generator
  adjusting grain size, shape and shape-axes orientation
constrained grain packer
  adjusting the spatial placement of grains
seed point generator-constrained Voronoi tessellation tool
crystallographic orientation assigner
  adjusting the bulk texture and boundary misorientation
Representative Volume Element (RVE)
Meso-structure Modelling
Notes: DREAM.3D generates 3D RVEs through four principal modules…
periodic boundaries

## Slide 13: Modelling and Simulation of Mechanical Response
Crystal Plasticity Simulations
Computation of
  constitutive mechanical response
  evolution and anisotropic interactions of the micro-state variables (MSVs) at the underlying deformation (slip/twin) systems of each grid/integration point of the RVE
via physics-based constitutive crystal plasticity model
MSVs
  unipolar dislocation density ()
  dipolar dislocation density ()
  twin (volume) fraction ()
at slip systems
at twin systems
Displacement-controlled uniaxial tension
Quasi-static strain rate ()
Room temperature ()
Notes: The macroscopic boundary conditions based upon homogeneous rate of the deformation gradient tensor and the first Piola-Kirchoff stress tensor with complementary components corresponding to uniaxial tension were applied.
unipolar (edge)  mobile
dipolar  immobile

## Slide 14: Modelling and Simulation of Mechanical Response
Good match between the experimental and simulated tensile curves
Mechanical response was successfully captured by the physics-based constitutive crystal plasticity model
Strain hardening curves
Flow curves
Crystal Plasticity Simulations
0° - orthogonal to building direction
45° - diagonal to building direction
90° - parallel to building direction
BD
S/TD
S.A.H. Motaman, F. Roters, C. Haase, Acta Materialia 185 (2020) 340–369.

## Slide 15: Modelling and Simulation of Mechanical Response
Tension - compression asymmetry
Different profile of stacking faults in compression and tension (orientation dependency of stress concentration on slip/twin systems)
Dependence of deformation twinning and martensite transformation on grain orientation and grain rotations during tension and compression
Strong texture formed during AM process
Internal shear mechanism of plastic deformation is sensitive to the sign of the shear stress
90° - parallel to building direction
BD
S/TD
0° - orthogonal to building direction
Notes: Interrupted mechanical tests are expected to give some valuable information to solve this issue.

## Slide 16: Lattice Structures
Mechanical behaviour
Cell design – f2cc,z
Specific energy absorption capacity in comparison to benchmark materials
Compression curves in comparison to benchmark materials
Mechanical behaviour under compression
P. Köhnen, S. Ewald, J.H. Schleifenbaum, A. Belyakov, C. Haase, Additive Manufacturing 35 (2020) 101389.
Notes: Different mechanical behaviour of different alloys (activating different deformation mechanisms)  interesting

## Slide 17: Lattice Structures
Cell design
Previous design: f2cc,z structure
S. Merkt, C. Hinke, J. Bültmann, M. Brandt, Y.M. Xie, Journal of Laser Applications 27 (2015) S17006.
schematic view
2D design
printed part
Drawback
Strain localization at z-strut nodes (parallel to load direction) under compression
Notes: Which is also the case for the TWIP steel with 1% Al, but of course with lower fraction of martensite

## Slide 18: Lattice Structures
Optimization of cell design
Curvy vertical struts (parallel to loading direction) instead of flat ones as main load carriers
Under compression, better distribution of the load along orthogonal directions
Less force exerting on the nodes
Preventing localization of strain and formation of brittle martensite phase at the early stages of deformation
3D design
variation of f2cc,z
f2cc,z
Current alternative

## Slide 19: Lattice Structures
Cell Design | Strut diameter (mm) | Unit cell edge length (mm) | Relative density (%)
Variation 1 | 0.8 | 3 | 12
Variation 2 | 1.0 | 3 | 19
Variation 3 | 1.25 | 3 | 28
Variation 4 | 1.5 | 3 | 37.5
Variation 5 | 2.0 | 3 | 58.3
In order to investigate the effect of relative density on compression / energy absorption behaviour
Optimization of cell design
1
2
3
4
5
density of the lattice structure
theoretical density of the bulk material
Notes: Studies shows that energy absorption capacity increases with increasing relative density

## Slide 20: Conclusion
Additively manufactured (LPBF) HMnS show microstructural heterogeneities which distinguish them from conventionally produced HMnS.
These heterogeneities (regarding crystallographic texture and grain size and morphology) can be included in the RVE generated by DREAM.3D.
Physics-based constitutive model (DisloTwin) can sufficiently capture the anisotropic mechanical response of HMnS.
HMnS lattice structures exhibit improved weight-specific energy absorption capacity in comparison to benchmark materials.
Cell design of the lattice structures needs to be modified in order to utilise TWIP effect.
Notes: Experience gained in the bulk material can be transferred to the lattice structures.

## Slide 21: Outlook
Finite element (FE) simulations of lattice structures
User-defined material model implemented in user subroutine UMAT (User MATerial) in ABAQUS
Calibration of the input parameters based on experimental and computational data obtained from the bulk material
Applying Cazacu-Barlat model – Yield function
Test the model with the f2cc,z structures (already available experimental data)
Apply the model to the modified f2cc,z structures
S.A.H. Motaman, F. Kies, P. Köhnen, M. Létang, M. Lin, A. Molotnikov, C. Haase, JOM 72 (2020) 1092–1104.
Notes: Defining the load case properly is challenging for lattice structures.