## Slide 1
Development of a novel in- situ alloying 3D printing procedure
exemplified on the permanent magnetic Fe-Cr-Co alloy system
S. Arneitz, R. Buzolin, S. Rivoirard, C. Sommitsch MAMC 2021

## Slide 2: Table of Contents
Introduction
  Our machine
  In- situ alloying: a novel process
Development of the in- situ alloying process
  Melt Pool Studies
  Study on the Influence of Powder Quality
  Influence of printing parameters on the homogeneity
  Materials Characterisation
  Determination of the miscibility gap
  Magnetic measurements of selected samples

## Slide 3: Our machine: ORLAS Creator
Size: 0.9 x 0.9 x 2 m³
Weight: 470 kg
Power Consumption: 1.2 kW
Materials: Steel allloys, aluminum alloys, Titanium alloys, novel reactive and non- reactive materials except Mg
Minimum Powder Requirements: 100-200g (Melt Pool tests),
0.7-1.5 kg (Parameter Studies)
Build Volume: ⌀ 110mm x 100mm
Materials Properties are reproducible over the whole build volume!

## Slide 4: In- situ alloying: a novel technique
Mischen, 1h
Mischhilfe:
Edelstahlkugeln
Fe
Cr
Co

## Slide 5: Development of the in- situ alloying process

## Slide 6: Development of the Printing Process: Powders
Mo < 800nm
Co < 10µm
Fe
Cr
CoCr

## Slide 7: Melt Pool Studies: Implementation
Investigated Parameter | 
Laser Power / W | 25, 65, 105, 145, 190, 240
Speed / mm/s | 100, 300, 500, 700, 900, 1100, 1300
Layer height / um | 25
Spot size / um | 50

## Slide 8: Melt Pool Studies: Results

## Slide 9: Parameter Study: Sample Geometry

## Slide 10: Parameter Study: Densities

## Slide 11: Parameter Study: Porosity

## Slide 12: Parameter Study: Chemical Homogeneity
Parameter | 
Laser Power / W | 65, 105, 145, 190, 240
Energy Density / J/mm² | 1.60, 2.80, 4.00

## Slide 13: Parameter Study: Chemical Homogeneity – Code for the analysis

## Slide 14: Parameter Study: Chemical Homogeneity – Code for the analysis
1
2
1 fully homogenized reference
2 sample (Cr 65W ED400)
2
1
Frequency
Luminance value

## Slide 15: Parameter Study: Chemical Homogeneity – Code for the analysis
Luminance value
Frequency
Luminance value
Frequency

## Slide 16: Parameter Study: Chemical Homogeneity – Code for the analysis
value of
inhomogeneity
Luminance value
Frequency
Luminance value
Frequency
1
2
1 fully homogenized reference
2 sample (Cr 65W ED400)

## Slide 17: Parameter Study: Chemical Homogeneity
xy direction
xz direction

## Slide 18: Parameter Study: Chemical Homogeneity
Tm = 1907 ºC
Tm = 1538 ºC
Tm = 1495 ºC

## Slide 19: Materials Characterisation

## Slide 20: Materials Characterisation: Determination of the miscibility gap
275HV
~ 620 ºC
~ 660 ºC
Reference | Reported T
Minowa et.al.1 | ~660°C

## Slide 21: Materials Characterisation: Magnetic Measurements
Sample # | Laser power / W | Energy density / J/cm² | Heat Treatment
1 | 240 | 400 | AB – 640HT
2 | 240 | 400 | Hom – 640HT
3 | 240 | 400 | Hom – 510HT
4 | 240 | 160 | Hom – 640HT
5 | Repetition sample 2 |  | 
6 | Repetition sample 4 |  | 
Cooling rate: 26K/h
640ºC : 1h
510ºC : 1h
510ºC : 50h

## Slide 22: Materials Characterisation: Magnetic Measurements
Sample # | Laser Power [W] | Energy density [J/mm²] | Homogenisation | Heat treatment | µ0Hc (kA/m) | µ0Mr (T) | BHmax (kJ/m3) | Anisotropy
1 | 240 | 400 | No | 640HT | 22 | 0.42 | 0.08 | No
2 | 240 | 400 | 1100°C – 1h | 640HT | 19 | 0.47 | 0.08 | No
3 | 240 | 400 | 1100°C – 1h | 510HT | 1 | 0.10 | 0.08 | No
4 | 240 | 160 | 1100°C – 1h | 640HT | 19 | 0.52 | 0.08 | Yes

## Slide 23: Materials Characterisation: Thermal Stability of magnetic properties

## Slide 24: Materials Characterisation: Anisotropy of magnetic properties

## Slide 25: Outlook: In- situ alloying and magnetic alloys
Fe- Cr- Co system
High Entropy alloys:
  Fe-Cr-Co-Ni
  Fe-Cr-Co-Ni-Al
Shape memory alloys:
  Ni-Ti
  Ni-Ti-Zr
AlSi10Mg + additive
AA5024 + additive
Nd- Fe- B system (conventional and recycled powders)
10 mm

## Slide 26: Thank you for your attention