## Slide 1: Microstructure and mechanical performance of Sandvik Osprey Inconel 625 produced via laser powder bed fusion
Leandro Feitosa, PhD
R&D Engineer
ADDITIVE BY SANDVIK
PLAN IT – PRINT IT – PERFECT IT

## Slide 2: agenda
Introduction
  About Sandvik
  IN625 alloys
Powder characteristics
methodology
  Process and parameter development
  Post processing
Mechanical properties
ConclusionS

## Slide 3
NEATH, UNITED KINGDOM
GAS ATOMIZED POWDER MANUFACTURING BY SANDVIK
SANDVIKEN, SWEDEN
Notes: Introduction to Sandvik AM Powder production units
PU Neath
Particle size: 5 – 80 micron
8 Inert Gas Atomisation (IGA)
Argon and Nitrogen atomising
Powder sizing
One plant dedicated to Aluminium alloy powders
AS9100D (Aerospace)
PU Sandviken
Particle size: 20 – 200 micron
1 Vacuum Gas Atomisation (VIGA)
1 EIGA Titanium powder plant
Argon and Nitrogen Atomising
Powder sizing
AS9100D (Aerospace)
ISO 13485:2016 Medical Certification

## Slide 4
MORE THAN
2000
GRADES
FIRST YEAR OF POWDER SALES
1979
OSPREY® METAL POWDERS
OUR PROGRAM OF OSPREY® METAL POWDER INCLUDES:
Maraging steels; 18NI300 & MAR-60HRC
Tool steels; M2 & H13
Stainless steels; 17-4PH & 316L
Nickel free SS; X15 CrMnMoN 17-11-3
Low alloy steels
Duplex steels
Cobalt alloys
Copper alloys
Controlled expansion alloys
Soft magnetic alloys
Binary alloys
High temperature materials
Nickel-based superalloys
Aluminium alloys
Titanium alloys
WORLD LEADER
IN METAL POWDERS
Notes: Ti-6Al-4V was one of the first titanium alloys developed and remains the predominant titanium alloy in the aerospace industry, because of its balanced and robust property set.
CoCr alloy offer for Medtech

## Slide 5: The Inconel 625 alloy
The Inconel 625 is a nickel-based superalloy, used in different applications due to its high strength, corrosion resistance, good fabricability and weldability. The good mechanical properties are obtained from the solid solution strengthening of elements such as Mo and Nb.
The IN625 is a solid-solution matrix stiffened FCC alloy, which may contain carbides, inherent in this type of alloy. The carbides that can be found are MC, M6C (rich in Ni, Nb, Mo and C) and M23C6, a Cr-rich carbide that is usually present in solution-treated material at lower temperatures.
A disadvantage of this highly alloyed material is its difficulty in being machined, due to the high hardness, low thermal conductivity and high work hardening rates

## Slide 6: Vacuum atomization of in625
In625 powder morphology
Osprey® Alloy 625-AM is a nickel base precipitation hardened superalloy.
Manufactured by melting under vacuum as powder by Inert Gas Atomisation (VIGA).
Attractive mechanical properties at elevated temperatures up to ~540°C

## Slide 7: IN625 powder characteristics
VIGA
 | Flow time 50g (s) | Size by laser (µm)
VIGA | 3.4 (Carney) | d10=24.8 d50=36.8 d90=57.3
Notes: Leandro

## Slide 8: Methods
MATERIAL TESTED:
IN625 Osprey VIGA
 | %wt.
C | 0.022
N | 0.006
O | 0.0049
Al | 0.15
Si | 0.05
P | 0.003
S | 0.009
Cr | 20.83
Mn | 0.01
Fe | 3.85
Co | 0.01
Ni | 62.15
Nb | 3.83
Mo | 9.05
Ti | 0.1
MECHANICAL PROPERTIES:
Tensile (RT and 540 °C)
Impact toughness (RT)
Hardness
OPTIMIZATION OF PROCESS PARAMETERS
Renishaw AM400, 30µm layer thickness
High density and crack free
SEM CHARACTERIZATION:
Microstructure
Notes: Leandro

## Slide 9: Build Plate Setups
    1048°C / 1h -> AC
    1000°C / 1h -> AC
    1048°C / 1h -> WQ
Notes: Fabio

## Slide 10: As-built microstructure
Fine cellular microstructure with segregation of alloying elements along boundaries
Nb tend to segregate into inter-dendritic regions due to low solubility of these elements in the FCC matrix
Formation of phases such as Ni3Nb, Laves and Nb/Mo-based carbides and oxides common
Notes: Fabio

## Slide 11
1048°C_1h_AC
1048°C _1h_WQ
1000 °C _1h_WQ
Heat treated microstructure
Notes: Fabio

## Slide 12: Mechanical properties at RT
Rp0.2 (MPa) / Horizontal
1048 °C, 1h, AC
1048 °C, 1h, WQ
1000 °C, 1h, AC
UTS (MPa) / Horizontal
1048 °C, 1h, AC
1048 °C, 1h, WQ
1000 °C, 1h, AC
Impact toughness (J)
1048 °C, 1h, AC
As Built
1048 C 1h,
AC
1048 C 1h,
WQ
Hardness (HV0.5)
Chart: 
Midas Horizontal 1048 C, 1h, AC | 469.3857
Midas Horizontal 1048 C, 1h, WQ | 457.0333
Midas Horizontal 1000 C, 1h, AC | 590.1
Chart: 
| UTS (MPa) RT
Midas Horizontal 1048 C, 1h, AC | 911.1429
Midas Horizontal 1048 C, 1h, WQ | 910.6667
Midas Horizontal 1000 C, 1h, AC | 944.6667
Chart: 
| Rp 0.2 (MPa) 540 °C
VIGA Horizontal 1048 C, 1h, AC | 144.7
VIGA Vertical 1048 C, 1h, AC | 163.2
Horizontal
Vertical
Chart: 
| IN625S S1 | IN625S S 1048AC | IN625S SA 1048WQ
 | 298.8889 | 238.1 | 230.7
Notes: Eleonora

## Slide 13: Mechanical properties at 540 °C
Rp0.2 (MPa)
Horizontal
Vertical
Elongation (%)
UTS (MPa)
Chart: 
| Rp 0.2 (MPa) 540 °C
VIGA Horizontal 1048 C, 1h, AC | 340.8667
VIGA Vertical 1048 C, 1h, AC | 335.8
1048 °C, 1h, AC
Chart: 
| UTS (MPa) 540 °C
Midas Horizontal 1048 C, 1h, AC | 760.7333
Midas Vertical 1048 C, 1h, AC | 717.6667
Horizontal
Vertical
1048 °C, 1h, AC
Chart: 
| A Lo25 (%) 540 °C
Midas Horizontal 1048 C, 1h, AC | 50.3667
Midas Vertical 1048 C, 1h, AC | 54.4333
Horizontal
Vertical
1048 °C, 1h, AC
Notes: Eleonora

## Slide 14: summary
Advantages of Powder Metallurgy are well-established
  Manufactured using Clean Vacuum Induction Melting Technology
  Good morphology and flowability, resulting in high density
  parts after printing.
As-built microstructure showed to be a key factor for the microstructure evolution following different annealing conditions, as it controls the formation of δ-phase and oxides.
At 1048°C, higher tensile for air cooled specimens, due to higher fraction of secondary phases, while 1000°C poor recrystallization but high strength due to precipitation, internal stresses and grain size.
Impact toughness results indicate that secondary phases are more important than oxides. Dductility is still high despite their presence.
540°C tensile evidenced good level of strength and plasticity is maintained, with secondary phase precipitations playing a more significant role.

## Slide 15: Thanks for listening! Questions?
Notes: Eleonora