## Slide 1: Novel development of a NbC-containing powder metallurgical martensitic steel with outstanding tribocorrosion resistance
Isabel Hahn, Sabine Siebert, Werner Theisen, Sebastian Weber

## Slide 2: Outline
Introduction
Experimental
Results and discussion
Conclusion

## Slide 3: Introduction – Motivation and challenges
Tribology/Wear
Corrosion
Tribocorrosion
    Tribocorrosion: Interaction between wear and corrosion
      Wear affecting corrosion simultaneously corrosion affecting wear
      Complex phenomenon

## Slide 4: Introduction – Motivation and challenges
    Applications,
    where
    tribocorrosion occurs:
    seal-free bearings
    medical sector
    cutting tools
    Development
    of tribocorrosion resistant steels
    leads to…
    …sustainability.
    …raised efficiency.
    …increased service life.
source: Waldemar Link GmbH & Co. KG
source: von den Steinen GmbH & Co.KG
source: Schaeffler AG & Co. KG

## Slide 5: Introduction – Motivation and challenges
    Applications,
    where
    tribocorrosion occurs:
    seal-free bearings
    medical sector
    cutting tools
    Development
    of tribocorrosion resistant steels
    leads to…
    …sustainability.
    …raised efficiency.
    …increased service life.
source: Waldemar Link GmbH & Co. KG
source: von den Steinen GmbH & Co.KG
source: Schaeffler AG & Co. KG
    Wear- and corrosion resistant steels ≠ tribocorrosion resistant steels!
    Predominant: microstructure  Hard phases, alloying elements, chemical composition of the matrix…

## Slide 6: Introduction – Tribocorrosion resistant steels with NbC
    NbC-content > 3 vol.-%
    C-free powder
    graphite powder
    mixing
    encapsulation and evacuation
    HIP-process
    decapsulation
    Diffusion-alloying
     complex and expensive
    Advantages of NbC as hard phase
    High hardness >2000 HV
    Low solubility of Cr in NbC
    Low solubility of Nb in Fe-matrix
    Disadvantages of NbC as hard phase
    High affinity of Nb to C, formation of coarse primary carbides
     Liquid state processing  PM

## Slide 7: Introduction – Tribocorrosion resistant steels with NbC
    Advantages of NbC as hard phase
    High hardness >2000 HV
    Low solubility of Cr in NbC
    Low solubility of Nb in Fe-matrix
    Disadvantages of NbC as hard phase
    High affinity of Nb to C, formation of coarse primary carbides
     Liquid state processing  PM
    Aim: Development of a NbC-containing tribocorrosion resistant steel with reduced Nb- and C-contents for powder metallurgical production
    ü

## Slide 8: Outline
Introduction
Experimental
Results and discussion
Conclusion

## Slide 9: Experimental – Materials for tribocorrosion testing
    Hardened, low-tempered T = 180°C
[wt.-%] | C | Si | Mn | Cr | Mo | Ni | V | Nb | Co | N | Fe
K190 | 2.80 | 0.54 | 0.31 | 11.50 | 1.03 | 0.23 | 3.60 | - | 0.03 | - | bal.
M390 | 2.70 | 0.56 | 0.28 | 18.76 | 1.00 | 0.24 | 3.62 | - | 0.06 | 0.27 | bal.
Nb-PMmeltC | 0.51 | <0.10 | 0.07 | 12.50 | 3.90 | 0.20 | 0.02 | 1.80 | 1.50 | 0.12 | bal.
    3 different PM-steels:
      Wear resistant steel K190: 28 vol.-% carbides
      Wear- and corrosion resistant steel M390: 21 vol.-% carbides
      Newly developed steel Nb-PMmeltC: 2.5 vol.-% carbides
      Difference in carbide-content, -type, -size

## Slide 10: Experimental – Tribocorrosion testing
    Without corrosive attack
     pure wear
    With
    corrosive attack
     tribocorrosion
    Sliding wear
    (material loss)
    Corrosion
    (current density at OCP)
    Without
    sliding wear
    With
    sliding wear
    How does tribocorrosion affect wear resistance?
    How does wear affect corrosion resistance?
    Parameter:
      Surface pressure: 1920 MPa
      Counterbody: Si3N4
      Time: 30 min (sliding wear)
      Electrolyte: 0.9% NaCl-solution

## Slide 11: Outline
Introduction
Experimental
Results and discussion
Conclusion

## Slide 12: Results and discussion – Tribocorrosion behavior
How does tribocorrosion affect wear resistance?
    836±3 HV30
    839±5 HV30
    750±7 HV30
    Tribocorrosion resistance: K190 < M390 < Nb-PMmeltC  How does tribocorrosion occur?
    Sliding wear resistance: K190 > M390 > Nb-PMmeltC
       Carbide content, hardness

## Slide 13: Results and discussion – Tribocorrosion behavior
    Wear tracks after sliding wear with corrosive attack (tribocorrosion)
    K190 and M390
      Corrosive attack at Cr-rich carbides
      Removed carbides  3-body abrasive wear  tribological load is intensified
      K190: Corroding matrix facilitates the removal of the carbides
    Nb-PMmeltC
      Abrasive wear, marginally corrosion occurs
      NbC supports metal matrix
      Cr, Mo, N are distributed in
      the metal matrix  PREN

## Slide 14: Results and discussion – Tribocorrosion behavior
    Wear tracks after sliding wear with corrosive attack (tribocorrosion)
    Tribocorrosion occurs differently
    Influence of corrosion on wear resistance

## Slide 15: Results and discussion – Corrosion behavior
    Current density under sliding wear
      Corrosive attack increases  corrosion resistance decreases
      Negative influence on tribocorrosion resistance of the steels!
How does wear affect corrosion resistance?
    Corrosion resistance
    medium: 0.9% NaCl

## Slide 16: Outline
Introduction
Experimental
Results and discussion
Conclusion

## Slide 17: Conclusion
    Wear- and corrosion resistant steels ≠ tribocorrosion resistant steels
      Predominant: microstructure  Hard phase, chemical composition of the matrix…
      Tribocorrosion: Interaction between wear and corrosion
    NbC-containing steels have a high tribocorrosion resistance
      High hardness and fine dispersion of NbC in metal matrix  wear resistance
      Low solubility of alloying elements in NbC + distribution of Cr, Mo and N in metal matrix  corrosion resistance
    NbC-containing steels can be produced powder metallurgically, if Nb- and C-contents are low
      Large-scale industrial implementation is possible

## Slide 18
Thank you for your attention
and your questions!
M.Sc. Isabel Hahn
Faculty of Mechanical Engineering
Chair of Materials Technology
Universitätsstr. 150, IC 03-325
44801 Bochum
Mail: hahn@wtech.rub.de
This research was funded by the German Federal Ministry for Economic Affairs and Climate Action (BMWK).
Project no. FKZ 03 ET14774A-H (Poseidon II)