## Slide 1: Retained Austenite in Tool Steels
Christoph Oberroither

## Slide 2: Retained Austenite in Tool Steels
Why are we talking about retained austenite in high-alloyed tool steels ?
Martensite Start Temperature (Ms) and Finish Temperature (Mf) drops with increasing C- content
At C-contents of > 0,7% the Mf drops below Room –Temperature
When quenched down to room temperature, metastable retained austenite may remain in the microstructure
Complete transformation from austenite into martensite takes place if quenched below room temperature or under application of adequate mechanical load

## Slide 3: Retained Austenite in Tool Steels
How can we detect retained austenite ?
How can we avoid retained austenite ?
How does retained austenite effect our tool performance ?

## Slide 4: How can we detect retained austenite ?
Metallographic inspection
Measurement of the magnetic saturation
Phase quantification by electron backscatter diffraction
X-ray diffraction

## Slide 5: How can we detect retained austenite ?
BÖHLER K340 ISODUR
Hardened & tempered
RA 3.5 % (XRD)
BÖHLER K340 ISODUR
Hardened & tempered
RA 16 % (XRD)
BÖHLER K329
Hardened & tempered
RA 8 % (EBSD)

## Slide 6: How can we avoid retained austenite?
Sub-Zero treatment
Sufficient tempering
combination
Choosing correct hardening temperature
Avoiding delays between heat treatment steps

## Slide 7: How can we avoid retained austenite ?
X153CrMoV12
A Hardening 1070 °C
      30 min
T Tempering 510 °C
2 hrs
SZ Sub-Zero - 80 °C
30 min
Chart: Hardness (HRC)
| A | A+T | A+2x T | A+3x T | A+SZ | A+T+SZ | A+SZ+T
Ringversuch (5 vaHPM- Härtereien) -BÖHLER K110 Restaustenit(%) | 31.6 | 10 | 4.1 | 2.3 | 10 | 7.9 | 0.3
Ringversuch (5 vaHPM- Härtereien) -BÖHLER K110 HRC | 61.1 | 61 | 61.4 | 61.1 | 63.5 | 61 | 61.2

## Slide 8: How does RA effect our tool lifetime ?
• Tools increase in size and even crack
High volume of RA
• Tools are too small in size
Austenite
Martensite
ΔV ~ +3%

## Slide 9: How does RA effect our tool lifetime ?
Material: BÖHLER K110
(X153CrMoV12 / 1.2379 / D2)
Reason of failure: Growth of longitudinal and transverse dimensions in the range of 0.02 – 0.08% during service
Tool: Die plate for fine blanking
Dimensions: 124.5 x 24.5 x 320 mm
Plates manufactured from near net
shaped hot rolled & annealed bar material

## Slide 10: How does RA effect our tool lifetime ?
Heat treatment:
Hardening: 1070°C quenching to 70°C
Tempering: 3 x 500°C 3 - 4 h
Hardness 58,7 – 61 HRC
RA 18,3 %

## Slide 11: How does RA effect our tool lifetime ?
All samples show normal carbide size & distribution for a hardened and tempered microstructure
The carbide orientation is parallel to the length of the plates

## Slide 12: How does RA effect our tool lifetime ?
Growth of the die plate in service is related to stress induced transformation of retained austenite during service
Die plates still show considerably high amount of retained austenite which comes from inadequate heat treatment i.e. tempering
The reported multiple tempers at around 500°C did not transform the retained austenite after hardening

## Slide 13: How does RA effect our tool lifetime ?
Same hardness level:
Insufficient heat treatment
Correct heat treatment
Improvement of
performance & lifetime

## Slide 14: How does RA effect our tool lifetime ?
Material: HS 4-3-2 (W4Mo3Cr4VSi)
Heat treatment: not received
Reason of failure: Chipping during service
Tool: Cold forming punch

## Slide 15: How does RA effect our tool lifetime ?
EDM layer
Hardness 60 HRC
Hardened and insufficiently tempered Microstructure
Thermal affection of about 3 μm was detected.
remaining EDM-layers
Abrasive wear on cutting edges
RA = 41% which is very high and not typical

## Slide 16: How does RA effect our tool lifetime ?
EDM surface supported the early fracture of the punches
Most likely the punches received only one temper at low temperatures which did not lead to transformation of retained austenite

## Slide 17: How does RA effect our tool lifetime ?
RA is regarded as a detrimental microstructural constituent when present in high-alloyed tool steels
It is difficult to determine small volumes of RA (LOM)
A reliable method for determining the volume of RA in high-alloyed tool steels is
X-ray–diffraction
RA can be the root cause of unexpected fatal tool fracture or dimensional instability of tools in service
Unfavourable amount of retained austenite in high-alloyed tool steels can be avoided by Sub-Zero treatments or by multiple tempering at temperatures sufficiently above the secondary hardening peak
Choosing an adequate heat treatment improves the tool- & high-speed steel’s properties and leads to an increase in tool lifetime and higher performance levels

## Slide 18: THANK YOU VERY MUCH FOR YOUR ATTENTION
Christoph Oberroither