## Slide 1: Title: Dry sliding tribological behaviour of cryotreated Cr-V ledeburitic tool steel against CuSn6 counterpart
Authors: Venu Yarasu, Peter Jurci, Jakub Hornik.

## Slide 2: 1. Introduction
Cr-V ledeburitic tool steel
Also known as Vanadis 6
Fabricated by PM route
Popular in Cold Work applications
Supplied in soft annealed condition
Applications:
Failures or Wear types:
1. Abrasive
2. Adhesive or Galling
Source: UDDEHOLM TOOL STEELS
Source: UDDEHOLM TOOL STEELS
Powder compaction
Blanking
Punches, etc
Source: IndiaMarket
3. a combination of both
Motivation

## Slide 3: 1. Introduction: Heat treatment
Conventional Heat-treatment
Cryogenic Treatment
CHT
CT
Temperature
Time
Austenitization
Vacuum gas quenching
Tempering
Tempering
Cryogenic Treatment
Temperature
Time
Austenitization
Vacuum gas quenching
Tempering
Tempering
Advantages of CT:
Reduction of retained austenite (γR) amount.
Refinement of martensite.
Increase in population density of small globular carbides (SGCs).
And finally, increase in the amount of nano-sized transient carbide precipitates.
Concern of CHT:
Higher amounts of retained austenite (γR).
About 20-30 %.

## Slide 4: 2. Material and Treatments: Process conditions
Hardening
Double Tempering
Cryogenic treatment
Material composition
%C | %Si | %Mn | %Cr | %Mo | %V | Fe
2.1 | 1.0 | 0.4 | 6.8 | 1.5 | 5.4 | Bal.
-75 °C
-140 °C
-196 °C
170 °C
530 °C
2 hrs
30 mins
17 hrs
Austenitization
1050 °C
Gas quenching
5 bar

## Slide 5: 2. Material and Treatments: Microstructure
Microstructure after tempering at 170 °C
Microstructure after tempering at 530 °C
-75 °C
-75 °C
a)
SCs
ECs
SGCs
TM
b)
SGCs
SCs
ECs
TM
TM: Tempered martensite
SCs: Secondary carbides (M7C3, Cr-rich)
ECs: Eutectic carbides (MC, V-rich)
SGCs: Small globular carbides (M3C, cementite)

## Slide 6: 2. Material and Treatments: Hardness
Mean Hardness
Change over CHT
HV.10
%
Chart: 
| CHT | CT, -75 °C | CT, -140 °C | CT, -196 °C
Tempered at 170 °C | 832 | 894 | 905 | 858
Tempered at 530 °C | 752 | 747 | 706 | 731
Chart: 
| CT, 75 °C | CT, -140 °C | CT, 196 °C
% Change, 170 °C | 7.45 | 8.8 | 3.1
% Change, 530 °C | -0.66 | -6.1 | -2.8
STD.D
Range: ± 2-6

## Slide 7: 2. Material and Treatments: Small Globular Carbides (SGCs)
Population densities of SGCs (x1000 mm-2)
Improvement over CHT in %
Chart: 
| CHT | CT, -75 °C | CT, -140 °C | CT, -196 °C
Tempered at 170 °C | 38.6 | 121.9 | 167 | 110
Tempered at 530 °C | 27.5 | 93.3 | 159 | 80
Chart: 
| CT, 75 °C | CT, -140 °C | CT, 196 °C
% Improvement, 170 °C | 215.8 | 332.6 | 185
% Improvement, 530 °C | 239.3 | 478.2 | 190.9
STD.D
Range: ± 0.4-2.8
Source:
Materials Characterization 134 (2017) 398–415
Vacuum 170 (2019) 108977 & Materials 2019, 12, 3827

## Slide 8: 3. Experimental Procedures
01
02
03
04
PIN-ON-DISK WEAR TESTING
CuSn6 6 mm diameter balls
Sliding distance of 100 Meters
Dry sliding wear tests at room temperature
OPTIMIZATION TECHNIQUE
Taguchi Method
L18 orthogonal design
Lower the better quality
CONTROL FACTROS
Cryogenic temperature
Tempering temperature
Sliding velocity
Load
FACTOR LEVELS
Mixed levels
Level | Tempering temp (°C) | Sub-zero temp (°C) | Sliding velocity (m/s) | Load (N)
1 | 170 | -75 | 0.064 | 1
2 | 530 | -140 | 0.128 | 5
3 |  | -196 | 0.1885 | 10

## Slide 9: 4. Results
Friction Coefficient (µ) – Response 1
Adhesion (% ) – Response 2
Friction Coefficient (µ)
Where:
F = Frictional force
N = Normal applied load
Estimated on:
12 random SEM images of wear tracks
Area % covered by counterpart material

## Slide 10: 4. Results: Normality tests
Friction Coefficient (µ)
Adhesion (%)

## Slide 11: 4. Results: SN Ratios
Experimental Result's
Main Effects Plot for SN ratios
FC
FC
Tempering (°C) | Cryotreatment (°C) | Sliding Velocity (m/s) | Load (N) | Friction Coefficient (µ)
170 | -75 | 0.064 | 1 | 1.107
170 | -75 | 0.128 | 5 | 0.904
170 | -75 | 0.1885 | 10 | 0.834
170 | -140 | 0.064 | 1 | 0.932
170 | -140 | 0.128 | 5 | 0.889
170 | -140 | 0.1885 | 10 | 0.875
170 | -196 | 0.064 | 5 | 0.932
170 | -196 | 0.128 | 10 | 0.880
170 | -196 | 0.1885 | 1 | 1.016
530 | -75 | 0.064 | 10 | 0.941
530 | -75 | 0.128 | 1 | 1.015
530 | -75 | 0.1885 | 5 | 1.015
530 | -140 | 0.064 | 5 | 0.985
530 | -140 | 0.128 | 10 | 0.939
530 | -140 | 0.1885 | 1 | 0.974
530 | -196 | 0.064 | 10 | 0.938
530 | -196 | 0.128 | 1 | 0.935
530 | -196 | 0.1885 | 5 | 0.959

## Slide 12: 4. Results: ANOVA
ANOVA Table
Significant Factors [p<0.05]
FC
FC
Source | DF | Seq SS | Adj SS | Adj MS | F | P | %C
TT | 1 | 0.5934 | 0.5934 | 0.5934 | 2.84 | 0.123 | 10.3
CT | 2 | 0.2996 | 0.2996 | 0.1498 | 0.72 | 0.512 | 5
Sv | 2 | 0.5106 | 0.5106 | 0.2553 | 1.22 | 0.335 | 9
L | 2 | 2.2564 | 2.2564 | 1.1282 | 5.39 | 0.026 | 39.2
Residual Error | 10 | 2.0914 | 2.0914 | 0.2091 |  |  | 
Total | 17 | 5.7514 |  |  |  |  | 
NOTES
DF: degrees of freedom
Seq SS: Sequential sum of squares
Adj SS: adjusted sum of squares
F: statistic
P: probability
Chart: 
| Load (N) | Tempering temperature (°C)
Contribution % | 39.2 | 10.3

## Slide 13: 4. Results: X-ray Spectroscopy
EDS Map after tribo-test at 1 N
EDS Map after tribo-test at 10 N
FC
FC
Process
CT: -196 °C
Tempering treatment: 530 °C
Process
CT: -75 °C
Tempering treatment: 170 °C

## Slide 14: 4. Results: SN Ratios
Experimental Result's
Main Effects Plot for SN ratios
Adhesion
Adhesion
Tempering (°C) | Cryotreatment (°C) | Sliding Velocity (m/s) | Load (N) | Adhesion (%) | Std.E
170 | -75 | 0.064 | 1 | 37.0 | 5.0
170 | -75 | 0.128 | 5 | 90.9 | 1.8
170 | -75 | 0.1885 | 10 | 93.2 | 0.6
170 | -140 | 0.064 | 1 | 61.0 | 2.7
170 | -140 | 0.128 | 5 | 90.3 | 1.6
170 | -140 | 0.1885 | 10 | 97.3 | 0.5
170 | -196 | 0.064 | 5 | 71.7 | 2.2
170 | -196 | 0.128 | 10 | 95.2 | 0.7
170 | -196 | 0.1885 | 1 | 18.6 | 1.0
530 | -75 | 0.064 | 10 | 60.3 | 3.1
530 | -75 | 0.128 | 1 | 27.2 | 1.3
530 | -75 | 0.1885 | 5 | 51.0 | 4.5
530 | -140 | 0.064 | 5 | 27.4 | 2.5
530 | -140 | 0.128 | 10 | 88.0 | 0.8
530 | -140 | 0.1885 | 1 | 23.8 | 1.3
530 | -196 | 0.064 | 10 | 61.4 | 4.4
530 | -196 | 0.128 | 1 | 12.5 | 0.7
530 | -196 | 0.1885 | 5 | 53.3 | 1.6

## Slide 15: 4. Results: ANOVA
ANOVA Table
Significant Factors [p<0.05]
Adhesion
Adhesion
Source | DF | Seq SS | Adj SS | Adj MS | F | P | %C
TT | 1 | 92.071 | 92.071 | 92.071 | 10.27 | 0.009 | 18.0
CT | 2 | 24.271 | 24.271 | 12.136 | 1.35 | 0.302 | 4.7
Sv | 2 | 3.657 | 3.657 | 1.828 | 0.2 | 0.819 | 0.7
L | 2 | 302.303 | 302.303 | 151.152 | 16.87 | 0.001 | 59.1
Residual Error | 10 | 89.621 | 89.621 | 8.962 |  |  | 
Total | 17 | 511.924 |  |  |  |  | 
NOTES
DF: degrees of freedom
Seq SS: Sequential sum of squares
Adj SS: adjusted sum of squares
F: statistic
P: probability
Chart: 
| Load (N) | Tempering temperature (°C)
Contribution % | 59.1 | 18

## Slide 16: 4. Results: Exposed Surface Analysis
Figure: Plan-view SEM micrographs showing exposed surfaces of specimens treated at temperature of -75°C, and tempered at 170 °C after testing at (a) 1 N, (b) 5 N, and (c) 10 N, tempered at 530 °C (d) 1 N, (e) 5 N, and (f) 10 N.
- With increase in load, adhesion increase irrespective of SZTs.
- Adhesion decreases when higher tempering temperature used (530°C)

## Slide 17: 5. Conclusions
Cryogenic treatment at -140°C followed by tempering at 170°C obtained higher hardness values.
Cryogenic treatment at -140°C followed by tempering at 530°C produced the lower hardness values.
Tempering temperature (170 °C), sub-zero temperature (-140 °C), sliding velocity (0.128 m/s), and load (10 N) are the best factors for friction coefficient.
  Due to, formation of continuous oxidized adhesive layer which may act as a lubricant.
The only significant factor for friction coefficient is load (39.2 %); however, tempering temperature contributes (10.3 %).

## Slide 18: 5. Conclusions
For counterpart adhesion, the optimum settings were: tempering temperature (530 °C), sub-zero temperature (-196 °C), sliding velocity (0.1885 m/s), and normal load (1 N).
  Mainly, attribute to lower hardness and population densities of small globular carbides (SGCs) when tempered at 530°C.
Load (59.1%) is the main significant factor for adhesion which is having highest contribution, followed by tempering temperature (18%).

## Slide 19
Thank you for your attention!