## Slide 1: Direct energy deposition of H13 tool steel on CuBe alloy substrate
Zhao Zhao, Massimo Pellizzari, Matteo Perini, Paolo Bosetti
UNIVERSITÀ DEGLI STUDI DI TRENTO
Department of Industrial Engineering

## Slide 2
Motivations & benefits

## Slide 3: 1. Background and motivations
Mold
Innovational design of plastic injection mold
Direct energy deposition (DED)

## Slide 4: 1. Background and motivations
Copper-Beryllium alloy
H13
Copper-Beryllium alloy
H13
Redesign
DED
Properties of mold materials
 | Hardness HV0.1 | Wear Resistance | Corrosion Resistance | Thermal Conductivity W/m.K
H13 | 800 | Excellent | Poor | 26
CuBe | 400 | Medium | Excellent | 145
Chart: 
| Cost | Lifespan | Production efficiency
H13 | 4 | 5 | 2
H13-CuBe | 7 | 5 | 6
CuBe | 9 | 3 | 7
Schematic of the H13 tool steel cladded mold
Comprehensive comparison of molds

## Slide 5: 2. Load-bearing capability
4 mm cladding
CuBe
H13
CuBe
4 mm
20 mm

## Slide 6: 3. Thermal conductivity
t
s
[1]
: the mean value of thermal conductivity of multi-material structures
: the thickness of material t, s, and c
: the thermal conductivity of material t, s, and c
[1] Zhang X, Sun C, Pan T, et al. Additive manufacturing of copper–H13 tool steel bi-metallic structures via Ni-based multi-interlayer[J]. Additive Manufacturing, 2020, 36: 101474.
c
500C
H13
CuBe

## Slide 7: 4. Balance between lifespan and productivity
Load-bearing capability
Thermal conductivity
H13 Cladding thickness ratio
Notes: A BOX, REMVOE

## Slide 8
Challenge: cracking elimination

## Slide 9: 5. Cracking elimination – Substrate preheating
5-layer H13 cladding using substrate preheating at 250C
H13
CuBe
Average hardness of CuBe
Over aging
Single-layer H13 without preheating
Single-layer H13 with 250 preheating
Notes: CHANGE SINGLE LAYER
MOVE SOME CURVE

## Slide 10: 6. Experimental design – clues from preheating
Hot cracking?
Cold cracking?
Reduction of thermal stress during solidification
Avoiding of volumetric change induced by martensite transformation during deposition
Main driver?
Preheating:

## Slide 11: 7. Cracking investigation – SS316 buffer
CuBe Substrate
SS316L
CuBe Substrate
H13
SS316L
Less thermal stress
Single layer
Double layer
No martensite transformation in SS316
Verifying the cracking mechanism
Similar coefficient of thermal expansion: SS316 vs CuBe
H13
SS316L
Martensite transformation plays no role on cracking

## Slide 12: 7. Cracking investigation – H13 vs SS316L
SL-2 SS316L cladding
DL-5 H13 cladding

## Slide 13: 7. Cracking investigation – existence of liquid film
Cu
Cr
Fe
EDS map in H13 cladding

## Slide 14: 7. Cracking investigation – dimensionless cracking index
Cu concentration increases
Cu concentration increases
Crack free
SS316
H13
Notes: CHANGE THE PLOT

## Slide 15: 7. Cracking investigation – Clues
Cracking exists both in SS316 and H13
The cracking tendency in SS316 and H13 is similar
Cracks are located at solidification grain boundaries
Existence of liquid film
Martensite transformation has no effect on cracking
Main elements are Fe and Cu
Cracks occur during solidification in the liquid state
Solidification cracking

## Slide 16: 7. Cracking investigation – cracking tendency
Solidification temperature range
Terminal liquid

Terminal liquid 
Cracking tendency 
Scheil solidification model – Fe-Cu binary system
40Fe-60Cu
Kou S. A criterion for cracking during solidification[J]. Acta Materialia, 2015, 88: 366-374.

## Slide 17: 7. Cracking investigation – the effect of Cu composition
Crack-free
Crack
Cu wt% |  |  | Cracking tendency
<5 | low | low | low
20 ~ 50 | high | low | high
>50 | high | high | low
Cu wt% |  |  | Cracking tendency
<5 | low | low | low
20 ~ 50 | high | low | high
>50 | high | high | low

## Slide 18: 8. Cracking investigation – conclusion
Direct joint
Functionally graded material
Pure Ni buffer

## Slide 19
Thank you for attention!
Zhao Zhao
PhD student
University of Trento
Email: zhao.zhao@unitn.it
UNIVERSITÀ DEGLI STUDI DI TRENTO
Department of Industrial Engineering

## Slide 20: Cracking investigation – Dimensionless cracking index
=dimensionless cracking index
=linear density of cracking
=mean length of cracks
=number of cracks in measured length
=cracking length of the crack I
=measured length in the transversal cross-section.
Transversal cross-section of the single-layer SS316L
Transversal cross-section of the second-layer H13
SS316L
H13
SS316

## Slide 21: Cracking investigation – Solidification cracking model
Kou S. A criterion for cracking during solidification[J]. Acta Materialia, 2015, 88: 366-374.
: local strain
: solidification shrinkage
: temperature
: time
: effective volume fraction of solid
: liquid flowing velocity at the grain boundary.
(Separation)
(Growth)
(Feeding)

## Slide 22: Cracking investigation – grain growth investigation
The channel length is proportional to solidification temperature range
, can represent the extent of liquid feeding and approximate the half of liquid channel width