## Slide 1: Plasma Nitriding Properties of Sintered Body Formed Using CoCrFeNiMn High-Entropy Alloy Powder by Varying Ball-Milling Duration
Kansai University
Functional Materials Lab.
1Graduate School of Science and Engineering,
2Department of Chemistry and Materials Engineering,
Facultry of Chemistry, Materials and Bioengineering,
Kansai University, Osaka, Japan
〇Jiaxin Peng1 and Akio Nishimoto2
Notes: Thank you for Mr. chairman
I’m Peng Jiaxin of Kansai University in Osaka, Japan.
Now, I’d like to talk to you about Plasma Nitriding Properties of Sintered Body Formed Using CoCrFeNiMn High-Entropy Alloy Powder by Varying Ball-Milling Duration.

## Slide 2: Background
1) G. Li, et al. : Scr. Mater. 191 (2021) 196-201.
2) T. Karimoto and A. Nishimoto, Metals. 10 (2020) 761.
After ball milling a CoCrFeMnNi gas-atomized powder, a sintered body was prepared by the SPS method followed by plasma nitriding, and the characteristics of the surface nitrided layer were evaluated.
Experimental object
Fig. XRD pattern of plasma-nitride HEAs 2)
Dislocations were introduced on the surface of an CoCrFeMn alloy powder by ball milling, and a simultaneous improvement in the strength of the sintered body and strain hardening occurred. 1)
Another study revealed that an expanded fcc structure formed on the surface of Cantor alloy during plasma nitriding at 673 K. 2)
short-time processing
energy saving
five or more metallic elements
in the range of 5-35 at%
a single-phase solid solution
low hardness of Cantor alloy with fcc structure
short-time processing
Easy control of temperature, time, atmosphere and pressure
uniform heating
increase of nitriding supply
High entropy alloy
Spark plasma sintering
Plasma nitriding
S-DCPN
Notes: Recently, high-entropy alloys have been developed, and they are known to three points.
The advantage of SPS is easy control of temperature, time, atmosphere and pressure. Improving the hardness of soft HEAs is extremely important, and one method is the surface treatment.
This figure shows a schematic of the plasma nitriding. S-DCPN has the advantages of uniform heating and increase of nitriding supply.
Recent years, a study found that dislocations were introduced on the surface of this HEA powder by ball milling and another study revealed that an expanded fcc structure formed on the surface of Cantor alloy at 673 K.
Experimental object on this study is shown in this.

## Slide 3: Experimental procedure
Milling time | 0, 5, 10, 15 h
Revolution | 300 rpm
Ball to powder ratio | 10 : 1
Solvent | n-Heptane
Atmosphere | Ar
Table 2 Conditions of ball milling.
Fig. 1 Schematic illustration of the setup for ball milling.
Material preparation
⇒Ball milling
SPS processing
Polishing
Plasma nitriding
Analysis
Element | Co | Cr | Fe | Mn | Ni
Nominal composition (at%) | 20.00 | 20.00 | 20.00 | 20.00 | 20.00
Particle size | 53 ~150 µm |  |  |  | 
Table 1 Gas atomizing powders.
Notes: Next, the experiment procedure is shown.
The starting material is gas atomized powder and Table 1 shows element composition and particle size. And conditions of ball milling are shown in Table 2.

## Slide 4: Experimental procedure
Heating time | 10 min
Sintering temperature | 1073 K
Sintering time | 10 min
Pressure | 50 MPa
Atmosphere | < 10-2 Pa
Table 3 Sintering conditions of SPS.
Fig. 2 temperature program of SPS.
Material preparation
⇒Ball milling
SPS processing
Polishing
Plasma nitriding
Analysis
Notes: After ball milling, powders were sintered by SPS and conditions of SPS are shown in Table 3.

## Slide 5: Experimental procedure
Nitriding temperature | 673 K
Nitriding time | 15 h
Total gas pressure | 200 Pa
Gas flow (N2 : H2) | 3 : 1
Screen | SUS316L
Table 4 Nitriding conditions of S-DCPN.
Fig. 3 Shape and size of sintered HEAs sample.
Material preparation
⇒Ball milling
SPS processing
Polishing
Heat treatment
⇒Nitriding (S-DCPN)
Analysis
Notes: At S-DCPN treatment, shape and size of sintered HEAs sample is shown in Figure 3 and nitriding conditions are shown in Table 4.

## Slide 6
poster
Results and Conclusion
XRD, SEM, FE-SEM, GD-OES, EPMA, Vicker Hardness, Wear test, Corrosion test
Notes: Experimental results and conclusion are announced with the poster.
Thank you for your kind attention.