## Slide 1
Kansai University
Effect of the Amount of Zr Addition on Microstructure and Mechanical Properties of CoCrFeNi High-Entropy Alloys Prepared by Mechanical Alloying and Spark Plasma Sintering
1Graduate School of Science and Engineering, Kansai University, Osaka, Japan
2Department of Chemistry and Materials Engineering, Kansai University, Osaka, Japan
〇ZiXiang Fan1 and Akio Nishimoto2
Notes: Thank you, Mr. chairman.
I’m Fan of Kansai University in Osaka, Japan.
Now, I’d like to talk to you about Effect of the Amount of Zr Addition on Microstructure and Mechanical Properties of CoCrFeNi High-Entropy Alloys Prepared by Mechanical Alloying and Spark Plasma Sintering.

## Slide 2
A multicomponent alloy obtained by blending of least five metals with compositions of 5%-35%
⇒The introduction of large lattice distortion makes it solid solution stable.
High Entropy Alloys(HEAs)
1. Introduction
(1) W. Huo, H. Zhou et.al Materials and Design 134 (2017), pp. 226-233
Stable phase is FCC phase.
High ductility
But
CoCrFeNiMn HEAs
Hardness (approximately 160 HV)
The hardness of CoCrFeNiZr-based alloys produced by the arc-melting method is approximately
150 HV to 550 HV.(1)
Notes: High Entropy Alloys (HEAs) is a multicomponent alloy obtained by blending of least five metals with compositions of 5%-35%. CoCrFeNiMn HEAs are typical HEA alloys. The stable phase of it is a single phase of FCC and has high ductility, but low hardness, approximately 160 HV. Arc melting is the typical method for making high-entropy alloys, but the hardness of CoCrFeNiZr alloys made by arc melting is also low, ranging from about 150 HV to 550 HV.

## Slide 3
CoCrFeNiZr alloy
‥ HEA with Zr added instead of conventional Mn
alloys are prepared by MA-SPS method
☞ Few reports of Zr addition to HEA
Mechanical alloying method
20 µm
Alloyed powders with fine and uniform solid solution can be produced by mechanically alloying pure metal powders
1. Introduction
Notes: So, in this study, HEA with Zr added instead of conventional Mn. Alloys are prepared by MA-SPS method CoCrFeNiZr alloys are prepared by the MA-SPS method to improve the mechanical properties of the alloys.

## Slide 4
Processing method
In the conventional sintering method, deterioration of the mechanical properties of the matrix due to prolonged high-temperature treatment has been a problem.
Spark plasma sintering （SPS） method capable of short processing time
Capable of producing sintered alloys with a dense and uniform microstructure
Diffusion by pulsed current acceleration effect is expected
Punch
Power source
Thermocouple
Pressure
Electrode
Electrode
Pressure
Spacer
Spacer
Punch
Sheet
Dies
Sheet
Pulsed current
Controller
‣ Atmosphere
‣ Temperature
‣ Pressure
‣ Time
Sample
Vacuum chamber
1. Introduction
Notes: The sps method allows sintering in a short time. Capable of producing sintered alloys with a dense and uniform structure.

## Slide 5
Powder
SPS processing
Polishing
Analysis
2 . Experimental procedure
Milling time | 50 h
Revolution | 300 rpm
Ball to powder ratio | 10 : 1
Solvent | n-Heptane
Atmosphere | Ar
 | Co | Cr | Fe | Ni | Zr
CoCrFeNi | 25 | 25 | 25 | 25 | 0
CoCrFeNiZr0.2 | 23.81 | 23.81 | 23.81 | 23.81 | 4.76
CoCrFeNiZr0.4 | 22.73 | 22.73 | 22.73 | 22.73 | 9.08
CoCrFeNiZr0.6 | 21.74 | 21.74 | 21.74 | 21.74 | 13.04
MA
Table 1. Powder composition (at%)
Table 2. Conditions of MA processing.
Notes: Next, the experimental procedure is shown here. Table 1 shows the composition of the powders. Table 2 shows the experimental conditions for MA.

## Slide 6
Temperature,T | 1273 K
Atmosphere | ≦10-2 Pa
Processing time | 8 min
Heating rate | 60 K / min
Pressure | 50 MPa
Powder
MA
Polishing
Analysis
2 . Experimental procedure
SPS processing
Table 3. Conditions of SPS processing.
Notes: Table 3 shows the experimental conditions for SPS. Sintering was performed at a heating rate of 60 Kmin-1 and at a sintering temperature of 1273 K for 8 min.

## Slide 7
Experimental results are announced with the poster.
Thank you for your kind attention.
Notes: Experimental results are announced with the poster.
Thank you for your kind attention.