## Slide 1
Novel additive manufacturing techniques:
Process development and manufacturing of a functionally graded structure
S. Arneitz, R. Buzolin, C. Sommitsch MAMC 2022

## Slide 2: AM of the Fe-Cr-Co alloy system: Using the in- situ alloying process to manufacture magnetic parts with a defined chemical gradient

## Slide 3: Content of our presentation
Additive Manufacturing of Fe-Cr-Co: process development
  (Melt pool studies)
  (Homogeneity analysis)
  Process Design
  Characterisation of the fabricated samples

## Slide 4: Fe-Cr-Co in the LPBF process
Fe-Cr-Co:
Semi- hard magnetic (~120kA/m)
Good printability
Strong tendency of single alpha phase formation

## Slide 5: In- situ alloying: a novel technique with high potential
Mixing, 1h
Mixing aid:
Stainless steel balls
Fe
Cr
Co

## Slide 6: Additive manufacturing of FeCrCo: Melt pool studies
Investigated Parameter | 
Laser Power / W | 25, 65, 105, 145, 190, 240
Speed / mm/s | 100, 300, 500, 700, 900, 1100, 1300
Layer height / um | 25
Spot size / um | 50

## Slide 7: Additive manufacturing of FeCrCo: homogeneity
Parameter | 
Laser powder / W | 65, 105, 145, 190, 240
Energy density / J/mm² | 1.60, 2.80, 4.00

## Slide 8: Additive manufacturing of FeCrCo: homogeneity
1
2
1 fully homogenized reference
2 sample (Cr 65W ED400)
2
1
Frequency
Luminance value

## Slide 9: Additive manufacturing of FeCrCo: homogeneity
Luminance value
Frequency
Luminance value
Frequency

## Slide 10: Additive manufacturing of FeCrCo: homogeneity
value of
inhomogeneity
Luminance value
Frequency
Luminance value
Frequency
1
2
1 fully homogenized reference
2 sample (Cr 65W ED400)

## Slide 11: Additive manufacturing of FeCrCo: homogeneity
xy direction
xz direction

## Slide 12: Additive manufacturing of FeCrCo: homogeneity
Tm = 1907 ºC
Tm = 1538 ºC
Tm = 1495 ºC

## Slide 13: Functional graduation
Introduction of a chemical gradient by LPBF

## Slide 14: Concept: Process Development

## Slide 15: Concept: Process Development

## Slide 16: Concept: Process Development

## Slide 17: Concept: Process Development

## Slide 18: Concept: Process Development

## Slide 19: Concept: Process Development

## Slide 20: Concept: Process Development

## Slide 21: Concept: Process Development

## Slide 22: Concept: Process Development

## Slide 23: Concept: Process Development

## Slide 24: Concept: Process Development

## Slide 25: Concept: Process Development

## Slide 26: Printing Parameter

## Slide 27: Results: Parameter 5

## Slide 28: Results: Parameter 5

## Slide 29: Results: Parameter 5

## Slide 30: Results: Parameter 5

## Slide 31: Results: Parameter 5

## Slide 32: First Results: Parameter 5

## Slide 33: First Results: Comparison of Parameters
380µm

## Slide 34: First Results: Comparison of Parameters
281µm

## Slide 35: First Results: Comparison of Parameters
453µm

## Slide 36: First Results: Comparison of Parameters

## Slide 37: First Results: Comparison of Parameters
231µm

## Slide 38: First Results: Comparison of Parameters

## Slide 39: Thank you for your attention!
Siegfried Arneitz
Graz University of Technology
Institute of Materials Science, Joining and Forming
Kopernikusgasse 24/I
Graz, Austria
0043 316 873 1656
Siegfried.arneitz@tugraz.at