## Slide 1: Forming of a cylindrical cup in 7075-T6 under warm temperature conditions
Sylvain Royne*, Hervé Laurent, André Maillard
* Speaker

## Slide 2: Context
Possibilities of application of ultra-high-strength alloys of new generation for parts of the car
[Hovorun et al. 2017]
Cost production
Weight
Security
Warm forming of Aluminium alloy 7075-T6
[R. Jini Raj et al.]

## Slide 3: Warm-forming of AA7075-T6
Heat treatment step
Best mechanical characteristics in T6 condition but low formability at
room temperature
250°C
Warm forming step
150°C
Warm forming of AA7075-T6
[Choi et al. 2019]
Tensile tests performed at 20°C and 200°C for different strain rates
[Kumar et al. 2014]
Notes: Interet warm forming comparer au hot forming

## Slide 4: Review of warm forming process
One-step production processes
Study an industrial warm forming process in two-steps with AA7075-T6
Warm forming of 7075-T6
Increase in formability with the temperature
Temperature limit at which formability decreases (220°C)
Best temperature of warm forming is around 200°C
[Huo et al. 2016]
[Wang et al. 2016]
Heating methods are not compatible with industry (between 5 and 10min heating time)
Warm forming of 6082-O in two-steps
No-isothermal condition
[Panicker et al. 2016]
Notes: Preciser pourquoi en 2 steps

## Slide 5: Contents
Experimental warm forming of a cylindrical cup in two steps
  Industrial warm forming device
  Experimental results
Numerical simulations of the forming
Results
Conclusion

## Slide 6: Industrial warm forming device : Blank heating tool
Front of the press
Back of the press
Blank
heating tool
Tool step 1
Tool step 2
Moving part of heating tool
Fixed part of heating tool
Heating rate : 400°C/s
Time to reach 200°C : 0.5s max
Blank h0 = 0.8mm
Ø157mm

## Slide 7: Industrial warm forming device : Tool step 1 and 2
Die
Punch
Blank holder
Stamped guide
Force sensor
Front of the press
Back of the press
Manual transfer
Pyrometer on the die to control the temperature of the blank during step 1 and 2
Thermocouple in all tools to control temperature
Clearance impose between the die and stamped guide
Tool step 1
Tool step 2

## Slide 8: Experimental conditions and results of punch reaction
Experimental step 1
Temperature of 20°C and 200°C
Clamping force of 41kN during step 1
Decrease in force reaction at 200°C
Temperature of the blank : -5°C from target temperature
Force deviation between +7kN and -2kN from the mean
Crack at 20°C
Experimental step 2
Temperature of 200°C
No clamping force during step 2
Temperature of the blank : -6°C from target temperature
Force deviation between +5kN and -2kN from the mean

## Slide 9: Numerical conditions of the warm forming process
2D axisymmetric model on Abaqus implicit-standard (elements CAX4)
Isothermal condition
Strain rate (,, , )
dependent Swift law identified with tensile tests at 200°C
Influence analysis of the friction coefficient on reaction force
Punch
Punch
Die
Blank holder
Die
Stamped guide
Fixed clearance
1mm
Step 1
Step 2

## Slide 10: Forming step 1 results
Friction coefficient of 0.08 seems to be the closest to experimental results
Friction coefficient of 0.10 can also be correct due to the deviation
Change in force direction observed numerically around 16mm of die stroke
Contact of the blank on the second punch radius
1st punch radius
2nd punch radius
Die
Blank holder
Notes: Mettre photo godet passe 1

## Slide 11: Forming step 2 results
Friction coefficients of 0.08 and 0.10 are in the force deviation
The start and end of the numerical reaction force is less consistent with the experimental results
First change in the curve : Die radius below the punch radius
Second change in the curve : Blank radius comes into contact with the die.
Punch
Die
Stamped guide
Punch
Die
Stamped guide
Punch
Die
Stamped guide
Third change in the curve : Blank radius is almost completely reduced to a straight line
Notes: Mettre photo godet passe 2

## Slide 12: Analyze
Friction coefficients of 0.10 or 0.08 is not good for the simulation
The coefficients found are low compared with those used in warm forming (0.15 – 0.20 or more)
Numerical simulations with a coefficient of 0.15 and 0.20 with variation of clamping force
  Hypothesis : interference between tool 1 and tool 2 due to the clearance imposed on tool 2 and all the clamping force is not applied
Clamping force of 20kN is the best fit with experimental result with a friction coefficient of 0.15
Clamping force of 15kN or less is the best fit with experimental result with a friction coefficient of 0.20
Variation of the friction coefficient depend of the pressure, velocity,…
Swift law is not representative of the behavior

## Slide 13: Summary
2 steps cylindrical cup forming possible at 200°C but crack at 20°C
Difficult to estimate the friction coefficient due to the force deviation
Change of reaction force direction more pronounced numerically
Outlook
  Measure experimental cylindrical cup thickness and strain to verify numerical simulations
Implement a friction model
Implement a new behavior law ( Voce, Mixed,…)

## Slide 14
Thank you for your attention
sylvain.royne@univ-ubs.fr herve.laurent@univ-ubs.fr andre.Maillard@cetim.fr

## Slide 15: Industrial warm forming device : Tool step 1
Die
Pyrometer
Blank-holder
Punch
Force sensor
Cartridge-heated tools
Thermocouple in every tool for control
Pyrometer to control blank temperature during forming

## Slide 16: Industrial warm forming device : Tool step 2
Die
Pyrometer
Stamped guide
Poinçon
Force sensor
Cartridge-heated tools
Themocouple in every tool for control
Pyrometer to control blank temperature during forming
No blank holder force applied during step 2

## Slide 17: Industrial warm forming device : Stamping range
157 diameter circular blank

## Slide 18
T6 heat treatment
Warm forming step
250°C
150°C