## Slide 1: Experiments and simulations of the drawing envelope of commercially-pure aluminum
Adrian J. Carter, Kelin Chen, Yannis P. Korkolis*
* Presenter

## Slide 2: Control in Forming – Industry 4.0
Allwood, J. M., S. R. Duncan, J. Cao, P. Groche, G. Hirt, B. Kinsey, T. Kuboki, M. Liewald, A. Sterzing, and A. E. Tekkaya. 2016. „Closed-loop control of product properties in metal forming“. CIRP Annals 65 (2): 573–96. https://doi.org/10/f85mbh.
Sensing – Decision Making – Actuating

## Slide 3: Cup-drawing for different BHF’s
Wrinkling
Ideal
Tearing
Wrinkling
Ideal
Tearing
BHF = 0 N
56 N
2090 N
978 N
1709 N
523 N
Optimal BHF = 470 N (Lange 1985)
Sample of Specimens AA1100-O, dia. 37mm

## Slide 4: Workability envelope
Adapted from M. Liewald
BHF
Drawing depth or
tearing
wrinkling
success

## Slide 5: Contents of this talk
Industry 4.0:
Sensing – Decision Making – Actuating
Identify the working envelope of the work material (AA1100) in 2 tempers
Establish a FE model that reliably predicts the working envelope.
This will identify the features that a “decision-making” model needs to have
(e.g., hardening, anisotropy, friction, element type & mesh, etc.)

## Slide 6: Cup-drawing Experiments

## Slide 7: Material
Aluminum Alloy AA1100, >99% Al (1% Si+Fe, 0.05-0.20% Cu, 0-0.5% Mn, 0-0.10% Zn)
0.51 mm thick
Blank diameters:
  35, 37 and 40 mm
Tempers:
  -H24 (Half-hard)
  -O (Fully annealed)
Ha et al., Mat’ls, 2020

## Slide 8: Former experimental apparatus for cup-drawing
30-Ton eccentric press (OBI)
Close-up of tooling
Table
Ram
1.5-inch pneumatic cylinders (x3)
Air line
Punch
Die
BH

## Slide 9: Current experimental apparatus for cup-drawing
Instron 8872 Servo-hydraulic Machine
25 kN Load Cell
108 mm stroke
Load
frame
Pneumatic pressure regulator
Drawing tooling
Load cell
Hydraulic actuator
Pneumatic cylinders (BHF)

## Slide 10: Modular cup-drawing tooling
Geometry of tooling
Exploded view of tooling
Punch
Blank holder
Die
Blank
R2
R2
tO=0.51
All units in mm
Ø 21.3
Ø 37
Ø 20

## Slide 11: Modular cup-drawing tooling
1.5-inch pneumatic cylinders
Punch
Die insert
Punch holder
Top plate
BH
Die holder

## Slide 12: Typical Punch Force-Displacement Curves

## Slide 13: 37 mm -O Punch Force vs Punch Displacement

## Slide 14: Workability envelope
Theoretical cup height

## Slide 15: Workability Envelope
SUCCESS

## Slide 16: Workability Envelope
SUCCESS

## Slide 17: Workability envelope, –O vs. –H24
SUCCESS

## Slide 18: Numerical simulations of cup-drawing

## Slide 19: FE Model
Blank-
Holder
Punch
Die
Blank
Amplified out-of-plane coordinates by 15 x
ABAQUS/Standard 2019 (implicit)
15,523 shell elements, linear, reduced integration (S4R)
von Mises (-H24) or Yld2000-2D (-O), Voce extrapolation
Soft contact (exponential) with finite sliding
Friction: punch-blank is 0.04, die-blank-blank holder is 0.17
Random 2% wrinkling imperfection on outer edge
3% imperfection added using cosine equation to facilitate necking
Δ

## Slide 20: FE prediction, wrinkling case

## Slide 21: FE prediction, successful case

## Slide 22: FE prediction, tearing case

## Slide 23: Workability envelope, exp. vs. FEA

## Slide 24: Workability envelope of –H24: exp. vs FEA

## Slide 25: Conclusions & Acknowledgements
Workability Envelope
Workability Envelope was established for AA1100-O and -H24 experimentally
Finite Element Modeling
Designed a shell model that can accurately predict wrinkling and tearing of cups
von Mises for –H24, Yld2000-2D for –O (ongoing)
FEA reasonably reproduces similar workability envelope compared to experiments
Acknowledgements
U.S National Science Foundation under award CMMI-1727490 (Joint NSF-DFG project)
Madison Chitwood, Chen Liu, Drew Havrilla, Matt Esser (OSU), Prof. Peter Groche, Alexander Breunig (PtU), Prof. Brad Kinsey, Prof. Jinjin Ha (UNH)

## Slide 26: Thank you for your attention. Questions?

## Slide 27: Experiments
40 mm
35 mm
37 mm

## Slide 30: F4 – Workability envelope

## Slide 31: Workability envelopes

## Slide 32: Workability envelopes

## Slide 34: Model Description
Ha et al., Mat’ls, 2020

## Slide 35: Onset of wrinkling (punch disp vs BH disp)

## Slide 38: 37 mm