## Slide 1: An efficient pre-hardened cryogenic forming process for AA7075 aluminum alloy sheets
B Feng*, H Y Jiang, B Gu, S H Li, Y T Qi
* Presenter

## Slide 2: (1) The development and lightweight demand of new energy vehicles
Development of Lightweight Technology for New Energy Vehicles in China
Sales of new energy vehicles

## Slide 3: (2) Future Development Trends of Lightweight Materials
Key Materials for Light Weighting |  |  |  |  | 
Material | Density (kg/cm3) | Compressive Strength (MPa) | Material Cost | Development in China | Outlook
Steel | 7.8 | 552 | Very Low | Widely used | ★
High strength Steel (HSS) | 7.85 | 1,379 | Low | Increasing | ★★★★
Al Alloy | 2.7 | 310 | Mid | Slow | ★★★★★
Mg Alloy | 1.74 | 275 | Mid | Slow | ★★
Carbon Fiber (CF) | 1.5 | 2,069 | High | Very Slow | ★
Aluminum alloy is a promising lightweight material for car bodies
Application of high-strength aluminum alloy to the B-pillar of NIO and Audi
NIO ES8
96.4% aluminum usage
Audi e-tron

## Slide 4: (3) The Challenge of Forming Process for high-strength aluminum alloy
Cold stamping
HFQ®
Severe cracking
Solution(40min)
Aging(12-24h)
Coarse precipitate within grains
Low efficiency and difficult organizational regulation
Unable to balance “high plasticity”, “high strength”, and “high efficiency” !

## Slide 5: (4) Potential development direction – cryogenic forming
Cryogenic properties of 2219 aluminum alloy
The principle of cryogenic forming for aluminum alloy thin-walled components
True stress (MPa)
True strain
Hardening doubled
60% increase in elongation
Blank holder
Die
Punch
Area B
Area A

## Slide 6: (5) Process principle of pre-hardened cryogenic forming
Pre-hardened cryogenic forming process (PCF)

## Slide 7: (6) Analysis of pre-aging system for PCF process
Pre-aging temperature / ℃ | Pre-aging time / Symbol | 
100 | 1h / PA-100-1h | -
120 | 1h / PA-120-1h | 3h / PA-120-3h
140 | 1h / PA-140-1h | -
DSC curves
Pre-aging process system of AA7075 aluminum alloy

## Slide 8: (6) Analysis of pre-aging system for PCF process
Influence of pre-aging system on cryogenic formability
Influence of pre-aging system on post-baking strength

## Slide 9: (7) PCF setup and procedure for W-shaped beam component
Cryogenic stamping system
W-shaped components
RT
PCF

## Slide 10: (8) Mechanical properties and thickness distribution
Post-baking strength
Thickness distributions

## Slide 11: (9) Conclusion
The plastic capability of pre-aged AA7075 alloys is improved at cryogenic temperature.
The mixed fine precipitates of GP zones and η' phases are relatively suitable for cryogenic deformation and PB process.
The W-shaped automotive component is successfully produced by PCF process, and the components exhibit good surface quality and thickness uniformity.

## Slide 12: Thanks!